# HEALING EFFICIENCY INDEX (HEI)

A Proprietary Unified Metric Combining Structural, Durability, and Functional Efficacy

## 1. Introduction

Self-healing concrete and cementitious composites require quantitative, unified performance evaluation beyond isolated recovery parameters. Existing studies typically report individual indicators such as stiffness recovery, crack closure, or permeability reduction, which do not provide a holistic measure of healing performance.

To address this limitation, the Healing Efficiency Index (HEI) is proposed as a proprietary, dimensionless, and unified metric that integrates structural resilience, durability restoration, and functional crack sealing into a single evaluative index.

## 2. Definition of Healing Efficiency Index (HEI)

HEI = 0.40 × (Er / E0) + 0.30 × (S0 / Sr) + 0.30 × (1 − wr / w0)

## 3. Description of Parameters

| Symbol | Description | Measurement Method |
| --- | --- | --- |
| E0 | Initial elastic modulus of undamaged specimen | Ultrasonic Pulse Velocity (UPV) |
| Er | Recovered elastic modulus after healing | Ultrasonic Pulse Velocity (UPV) |
| S0 | Initial water sorptivity | ASTM C1585 |
| Sr | Residual water sorptivity after healing | ASTM C1585 |
| w0 | Initial crack width | Optical microscope / calibrated caliper |
| wr | Residual crack width after healing | Optical microscope / calibrated caliper |

## 4. Performance Components and Weighting Rationale

Structural Resilience (40%): Quantified through elastic modulus recovery, representing the material’s ability to restore stiffness and load transfer.

Durability Restoration (30%): Evaluated using water sorptivity reduction, indicating improved resistance to moisture ingress and durability deterioration.

Functional Integrity (30%): Measured by crack width reduction, reflecting effective crack sealing.

## 5. Interpretation and Acceptance Criteria

HEI ≥ 0.70 : Effective self-healing – Acceptable
0.50 ≤ HEI < 0.70 : Partial healing – Conditional acceptance
HEI < 0.50 : Ineffective healing – Rejected

## 6. Advantages of the HEI Framework

- Unified assessment of self-healing performance
- Based on standardized and repeatable test methods
- Eliminates single-parameter bias
- Applicable for research, QA/QC, and performance-based specifications

## 7. Intellectual Property Notice

The Healing Efficiency Index (HEI) is a proprietary performance metric. The formulation, weighting scheme, and decision thresholds are original and intended for academic and research use with proper attribution.

## 8. Attribution

Invented by: Anil F. Dhobale
Ajinkya DY Patil College, Pune, India
Date: December 13, 2025